## Slide 1: Finite Element Analysis of a Compact Clamped-Clamped NEM Relay
Akash Levy
7/17/20
Analysis Updates

## Slide 2: Relay Thickness Dimensions: Parametrized

## Slide 3: Relay Components
Spherical Universe
Relay + Substrate
Substrate Components

## Slide 4: Meshing
Simple mesh vs. full mesh
Simple mesh uses swept surface mesh on substrate and poly-Si layers and free tetrahedral elements everywhere else
Full mesh uses free tetrahedral elements everywhere
Full mesh used for quick analyses
Simple mesh used for harder analyses

## Slide 5: Spring Constant Determination
Apply constant nodal force () across plate area and observe steady-state displacement ()
Hold anchors fixed against substrate (not shown)
Compute spring constant as:
Simplest hand calculation predicts:
    Beam equation where force is applied only at free end of beam
    Assuming entire beam is made of poly-SiGe and no bending of plate
    Not too far off! ANSYS had 25 N/m
Boundary Loads

## Slide 6: Stress and Strain
Elastic stress and strain can help us understand stressed locations
Can show points of possible relay fracture
Hot spots appear at corners
Generally look where differential bending is high
For a 1e-8 N force:
    Maximum stress:
    Maximum strain:

## Slide 7: Modal Analysis
Shows dominant modes of relay motion (rotational, flexural, etc.)
Way to understand relay motion and time constants
Can also extract spring constant from the first mode

## Slide 8: Modal Analysis
Shows dominant modes of relay motion (rotational, flexural, etc.)
Way to understand relay motion and time constants
Can also extract spring constant from the first mode

## Slide 9: Quasi-Static Analysis
Time-dependent analysis
Inertial terms ignored
Damping included to prevent instability of solution
Slowly sweep gate voltage (with relay grounded)
Observe steady-state displacement
Green curve: castor oil
Blue curve: vacuum/air

## Slide 10: Quasi-Static Analysis
Time-dependent analysis
Inertial terms ignored
Damping included to prevent instability of solution
Slowly sweep gate voltage (with relay grounded)
Observe steady-state displacement
Green curve: castor oil
Blue curve: vacuum/air

## Slide 11: Contact Force and Resistance Modeling
Contact cannot be directly modeled with built-in tool when an ambient is present (in both COMSOL and ANSYS
Ambient is required in COMSOL for electric fields to be modeled
Using penalty-based contact force (spring-based method)
Smoothed using exponential decay for convergence
Conserves system energy
Does this approach look valid?

## Slide 12: Contact Force and Resistance Modeling (previous)

## Slide 13: Contact Force and Resistance Modeling (previous)
Stdev Contact Force: 700nN, Stdev Intrinsic Contact Resistance: 1.4 Ω

## Slide 14: Contact Force and Resistance Modeling
Conclusion is that we need to optimize contact placement
We need multi-pole contact placement for uniform contact resistance
Strategy would be strong addition to a paper
UPDATE: Using rotational symmetry and extract rotation offset from displacement contour
Asperity-Based Contact Resistance Model

## Slide 15: Contact Force and Resistance Modeling (now)

## Slide 16: Contact Force and Resistance Modeling (now)
Stdev Contact Force: 15nN, Stdev Intrinsic Contact Resistance: 0.067 Ω

## Slide 17: Parasitic Extraction: Technique
Using stationary source sweep
Sets each of the 26 relay terminals to 1V and rest to ground
Relay terminal list:
    Gate on Substrate (x1)
    Relay Body (x1)
    Contact & Channel (x8)
    Landing Pads on Substrate (x16)
Models electric field inside spherical universe from earlier
Extracts mutual capacitance using matrix transformation on Maxwell capacitance

## Slide 18: PEX Results (OFF)
Air/Vacuum | Gate | Body | Landing Pad | Channel
Gate | 1.4e-16 F | 1.2e-15 F | 5.7e-16 F | 8.3e-18 F
Body | 1.2e-15 F | 3.2e-16 F | 7.0e-19 F | 1.2e-16 F
Landing Pad | 5.7e-16 F | 7.0e-19 F | 1.3e-19 F | ~0 F
Channel | 8.3e-18 F | 1.2e-16 F | ~0 F | ~0 F
Castor Oil | Gate | Body | Landing Pad | Channel
Gate | 4.2e-16 F | 3.2e-15 F | 5.7e-15 F | 4.3e-17 F
Body | 3.2e-15 F | 1.1e-15 F | 2.3e-18 F | 1.4e-16
Landing Pad | 5.7e-16 F | 2.3e-18 F | 7.4e-19 F | ~0 F
Channel | 4.3e-17 F | 1.4e-16 | ~0 F | ~0 F
All within a factor of 2 of parallel plate capacitor treatment!
For reference: 40nm minsize inverter capacitance is ~1e-16 F

## Slide 19: Modal Analysis with Viscous Damping
Material | Viscosity (Pa s) | Mode # | Damping ratio | Q factor
Air | 1.8e-5 | 1 | 5.9e-9 | 8.5e7
Air | 1.8e-5 | 2 | 1.0e-8 | 4.8e7
Castor Oil | 0.957 | 1 | 3.3e-4 | 1511
Castor Oil | 0.957 | 2 | 5.6e-4 | 893
We previously said these seemed unrealistic
Probably better to compute using a proper FEA simulation

## Slide 20: Transient Sweeps
25ns pull-in time without damping, 50ns with bounce
With damping in air: ~26ns
Viscous fluid damping
Unable to solve with castor oil for some reason
Will structural damping/dissipation play an important role in preventing contact bounce?
Displaying viscous laminar flow in air

## Slide 21: Other Configurations
2D modeling for damping coefficient extraction
Can assume ~0 pressure around perforations and assume thin-film flow (using Reynold’s equation)
Can also go and look at molecular flow regime
COMSOL has tools for both
On the right: perforated MEMS with computations damping coefficient computed

## Slide 22: ANSYS Plots From CFD
Velocity
Pressure
Pressure Contour

## Slide 23: Goal for SPICE Model
Ultimately, we want to work with reduced-order models suitable for SPICE simulation
Goal: extract key parameters that capture essence of FEA model
Possible simplified model of relay is shown below (from Berkeley)

## Slide 24: Updates on SPICE Model
Adapted a model found online
    Verilog-A Large-Signal RF MEMS Model Library
    http://rfmems.sourceforge.net/
    Removed a lot of unnecessary features
      (Brownian motion, RF-specific stuff)
High schooler (Akhilesh) created generators for multi-pole variant
Also developed and currently testing NEM multiplexer SPICE models
TODO: compare transient simulations across models

## Slide 25: Coming Up
Finalizing the fluidic stuff
Parasitic extraction in the ON state for validation
Transient simulation and comparison to SPICE model
Parameter sweeps (if time permits and it seems useful)

## Slide 26: Thank you!
Questions?